## Slide 1: Robert Goldstein, Fluxtrol, Inc. rcgoldstein@fluxtrol.com Ethan Buchner, Robert Cryderman Colorado School of Mines, Golden, Colorado
Modeling of Short Time Dilatometry Testing of High Carbon Steels

## Slide 2: Overview
Effect of Short Time Heat Treatment on Transformation Phenomena
  Test Results That Led to the Study
Dilatometer Description
Modeling Dilatometer Performance
Comparison Between Simulation and Experiments
Conclusions/Future Research

## Slide 3: Effect of Short Time Heat Treatment on Transformation Temperature
Superior Performance of Components Has Been Achieved in Many Cases Using Non-Equilibrium Thermal Processes (NETP), but There Is Very Little Quantitative Data Available on Material Response to Rapid Thermal Processing

## Slide 4: Recent Findings at ASPPRC of Improved Mechanical Properties with NETP
Up to 3X better properties demonstrated using appropriate alloying elements and relatively short, low temperature heat treatment

## Slide 5: Dilatometer Testing of the Steel for Materials Characterization
Effect of Reduced Pre-Transformation Expansion with Increasing Cooling Rate called Temperature Gradient Effect and Led to Impression There Was Non-Uniform Temperature in the Sample
Cooling Rates:
  He: 235 ˚C/s
  N: 91 ˚C/s
  Ar: 52 ˚C/s

## Slide 6: Dilatometer Description
Measures dimensional movement during thermal procession
Heating is in a vacuum
Heat source is induction heating
  Advertised heating rate up to 1000 C/s
Gas quenching through induction coil used for cooling
Fused silica rods hold the component
Manufacturer TA Instruments

## Slide 7: Modeling of Dilatometer Tests
Heating and Cooling simulations separated due to differences in enthalpy of phase transformations
1 D Program ELTA used initially to determine radial gradients and inverse calculations of material properties
2D Program Flux Used for Determining Full Temperature Distributions
For Flux – ½ of axisymmetric system used

## Slide 8: Comparison of ELTA with Experimental Data
Surface Temperature tracks closely
Dynamics of power change very similar
Big discrepancy in power level, measured substantially higher than calculated

## Slide 9: Radial Temperature Gradients for Different Heating Rates with Helium Quench
Chart: Radial Temperature Differential
For 50 CPS, radial gradients much larger during cooling than heating. As heating rate increases, gradients during initial heating approach those from the rapid cooling. After Curie Point, radial temperature difference close to 0 for all samples during heating and holding phase

## Slide 10: 2D Modeling with Flux
Axial Gradients are Larger than Radial Gradients on Heating According to Models
Axial Gradients Also Exist on Cooling, with ends being colder than center for uniform heat transfer coefficient on surface

## Slide 11: 3 TC Testing and Comparison to Models Heating
Experiments
Models

## Slide 12: 3 TC Testing Cooling Comparison
Experimental End to End
Experimental Cool End to Models
Axial Variation in Temperature is High, End to End Cooling Different, Initial Inversion Relative to Models Means We Have Significant HTC Variation in Length and Time!
Cool End
Hot End
Initial Inversion of Gradient Compared to Models
Excellent Agreement
During Heating

## Slide 13: Image During Cooling
Cool End
Hot End

## Slide 14: Conclusions
Models have been created to determine temperature distributions which occur during dilatometer testing
Once the steel started transforming from magnetic to non-magnetic, the generator power level rises dramatically, limiting the ability to deliver high heating rates
  Need to understand better as there is a significant variance from calculated power levels and need to determine how to increase power delivery
For rapid heating and cooling rates, there are significant gradients (both axial and radial) in the part which need to be considered when evaluating dimensional movement data
More work still needs to be done to better characterize/improve the cooling dynamics in the system